Installation Instruction for Profurl Screw’s (Extrusion Grub Screw’s and Locking Screw’s)

Installation Procedure.

- Dry assemble in factory to ensure all items included and correctly manufactured.

- Assembly at vessel, (or on factory floor for fitting to pre-assembled rigs):

- Ensure all parts are clean and dust free

- Using Loctite coat both the thread of the screw and the Extrusion/Turnbuckle Tube or Furler Mechanism thread, noting the Loctite working time available before setting.

- Install all screws only hand tight for stepping.

- When rig is stepped and tension is applied all furler screws need to be tightened to 5 N.m. (44 lbf.in) using bosuns chair as required for accessibility. Tightening must be completed before Loctite is set, re-coat if unsure.

- As extrusion screws are tightened, cover screw head flush to extrusion with supplied Sikaflex to form a seal of the screw. Must be flush and any excess cleaned away from extrusion/turnbuckle tube.

- Pre-assembled rigs to be taped to mast for transport, leave plastic cover on extrusions to provide protection against scratching.

- Advise owner not to sea-trial until after manufacturers advised 100% cure time of Loctite and Sika products (48 hours minimum).

- Have a beer and enjoy the afternoon.